## Slide 1
  Design for robotic welding, DFRW
Disclaimer
The European Commission support for the production of this publication does not constitute endorsement of the contents which reflects the views only of the authors, and the Commission cannot be held responsible for any use which may be made of the information contained therein​.​​​​​​

## Slide 2: DFRW: Basic prerequisites
  The designer must be more aware of the production
  Important with cooperation design-production
  Should the product be welded?
  Bending
  Casting
  Forging
  Gluing (Adhesive strength at least equivalent to Al)
  Riveting

## Slide 3: Extra important for robotic welding
The accessibility to the joint for the welding gun and safe distance to the robot depends on the design of the product.
Can the joint be reached?

## Slide 4: Extra important for robotic welding
Do the details have accurate tolerances?
A robot cannot compensate for dimensional deviations in the components involved and thus requires tighter tolerances
The right type of joint for robot welding?
Avoid welding near a bent radius. If the bending radius varies, the gap changes and the weld becomes incorrect.
Avoid Edge and Butt welds

## Slide 5: Extra important for robotic welding
Self-aligning parts simplify production.
Are the parts self-aligning – have well defined positions?
Design of built-in guide lugs and recesses
Steering towards other parts in at least three directions

## Slide 6: Right conditions for robotic welding
Does the construction have a weld-free side?
Positioners or manipulators require that the product has a weld-free surface for holding.
Design the product so that welding can take place in the horizontal plane.
Can the joint be welded horizontally?
Weld-free surface

## Slide 7: Product structure
Is the product divided into modules?
Modular construction provides better accessibility and often less deformation of the finished product
Is the number of components minimized?
Reduce the number of components e.g. by bending or other processing.

## Slide 8: Product structure
Is welding near shape-sensitive parts avoided?
Avoid welds near shape-sensitive parts. Threaded holes can be damaged if a weld is placed too close.
Place the weld where the load is lowest!
By placing the weld where the load is not high, the amount of weld and welding requirements can be reduced.

## Slide 9: Design
Is the amount of weld minimized?
Select the smallest possible throat thickness.
Max a6 can be placed with one string.
Possible with continuous weld with varying a-dimensions.
Intermittent or sometimes with spot or plug welds.
Use the penetration in fillet welds for reducing throat thickness.
Reduce the amount of welding by cutting complex contours.
Minimize the amount of welding, by bending, intermittent weld or cutting parts with complex geometry.

## Slide 10: Design
Do not take up tolerances in the weld joint!
Does the product have the “right” tolerances?
Too accurate tolerances means large costs in manufacturing
Do not allow that tolerances of parts to affect the position of the weld joint.

## Slide 11: Dimensioning
Is the lowest acceptable welding class used?
Occurrence of welding defects determine whether a weld meets the requirements for the specified welding class.
Do the parts have the same thickness?
Large dimensional differences lead to differences in cooling rate for the components during welding